## Slide 1: Interconversion between iron Oxides
Xiaozhe Zhang
09/21/2014

## Slide 2: Structures of Iron Oxides
α-Fe2O3
γ-Fe2O3
Fe3O4
 | α-Fe2O3 | γ-Fe2O3 | Fe3O4
Space group | R-3c (167) | Fd-3m (227) | Fd-3m (227)
Lattice constants | 5.0079 (A) | 8.3300 (A) | 8.384 (A)

## Slide 3: The interconversion of iron oxides
α-Fe2O3
γ-Fe2O3
Fe3O4
Reduce (I)
H2, thermal reduction
Oxidize(II), O2
α-Fe2O3 = 2/3 Fe3O4 + 1/6 O2 (I)
Fe3O4 + 1/4 O2 = 3/2 α-Fe2O3 (II)
Fe3O4 + 1/4 O2 = 3/2 γ-Fe2O3 (II)
γ-Fe2O3 = α-Fe2O3 (IV)
Structrue change, T (IV)
Oxidize(III), O2

## Slide 4: Interconversion in between of α‑Fe2O3 and Fe3O4
J. Phys. Chem. C 2014, 118, 29068−29076
FeO on Pt(111)
Fe3O4 film
α-Fe2O3 with structure
Fe3O4 and α-Fe2O3
LEED patterns of the surface structures
Crystal structures of FeO, wüstite (a), Fe3O4, magnetite (b), and α-Fe2O3, hematite (c).

## Slide 5: Interconversion in between different phase of Fe2O3
Chem. Mater. 2011, 23, 3255–3272

## Slide 6: Interconversion in between of α‑Fe2O3 and γ-Fe2O3
ACTA PHYSICA POLONICA A, 125 (2014)

## Slide 7: Interconversion in between of α‑Fe2O3 and Fe3O4
Langmuir 2011, 27(1), 11–14
Fe(110)
300 K
450 K
600 K
800 K
Fe(110)
Fe2O3(0001)
Fe3O4(111)
UPS
FeO(111)
FeO
Fe3O4
FeO
Fe3O4

## Slide 8: Summary
Describe the phase transition with different method, like XRD, XPS, LEED.
Lack of theoretic analysis
In our experiment:
Real time RHEED study of phase transition.
Thermodynamic analysis
hetero-multilayer growth of iron oxides.
Al2O3/α-Fe2O3, Al2O3/Fe3O4, Al2O3/Fe3O4/γ-Fe2O3, Al2O3/Fe3O4/ α- and γ-Fe2O3 biphase